## Slide 1: RDCH 702: Lecture 9 Separations
Separation methods
  Solvent extraction
    PUREX
  Ion exchange
  Electrochemistry
  Volatility
Specific actinide separations
Basic concept of separations
  Oxidation state
  Ionic radius
Development of advanced separations
  Trivalent actinides
Necessary for fuel cycle due to formation of mixtures due to fission
  Actinides
    Transuranics
  Fission products
    Se (Z=34) to Dy (Z=66)
Tributyl phosphate (TBP)

## Slide 2: Solvent Extraction
Two phase system for separation
  Sample dissolved in aqueous phase
    Normally acidic phase
Aqueous phase contacted with organic containing ligand
  Formation of neutral metal-ligand species drives solubility in organic phase
Organic phase contains target radionuclide
  May have other metal ions, further separation needed
    Variation of redox state, contact with different aqueous phase
Back extraction of target radionuclide into aqueous phase
  Reduction of Pu to trivalent
Distribution between organic and aqueous phase measured to evaluate chemical behavior

## Slide 3: Solvent extraction
Influence of chemical conditions
  Solvent
  Metal ion and acid concentration
    Phase splitting
Distribution coefficient
  Used to determine separation factors for a given metal ion
    Ratio of Kd for different metal ions
      May be represented by Kd or D
    Kd= 1
      50 % of metal in organic phase
    Kd= 10
      90.9 % of metal in organic phase
    Kd= 100
      99.01 % of metal in organic phase
  Distribution can be used to evaluate stoichiometry
    Evaluation distribution against change in solution parameter
      Plot log Kd versus log [X], slope is stoichiometry
Extraction can be explained by complexation
  Used to determine complexation constants

## Slide 4: Distribution coefficient and stoichiometry
Plot log Kd versus log [X]
  slope is stoichiometry of evaluated parameter
Consider reaction
  xM + yLMxLy
    Want to determine value for y
    Plot log Kd against log [L]
Use complexation constant and distribution coefficient
,
Substitute Kd into K equation, x=1
Log of equation
  Log K = log Kd – y log [L]; rearrange equation
  Log Kd = Log K + y log [L]
    Log K is constant
    Slope of log Kd versus log L gives y, the L stoichiometry

## Slide 5
Oxidation state importance
D variation with acid concentration

## Slide 6: Solvation Extraction Mechanism
CMPO
Extraction of neutral complex
  UO2(NO3)2 forms with TBP (P=O functional group)
    Equilibrium shifts with nitrate, back extraction into aqueous at low nitric acid
Other extractants include bifunctional ligands
  Carbamoyl phosphate compounds
    2 to 4 CMP per extracted molecule
  Carbamoylphosphine oxide (CMPO)
    2 CMPO for U and Pu, 3 for trivalents
      Basis of TRUEX separation for Ln/An
  Malonamide extracts can replace CMPO
    CHON principle
    DIAMEX process
Malonamide

## Slide 7: Ion Pair Formation
Charged metal complex with extractant of opposite charge
  Quaternary ammonium salt with anionic actinide nitrate
    R4N+
    Aliquat 336
  Tertiary amines
    R3HN+AnXn-(n-z) for monovalent X with An with Z charge
      Require equilibration with acid
Can be sorbed to resins for separations
  TEVA resins

## Slide 8: Liquid cation exchanger and chelating agents
Metal ion exchanged into organic phase, ion transfer in aqueous phase
Use of organic soluble acid
  i.e., alkyl phosphinic acid (R2PO2H)
Can be controlled by acidity
May form aggregates or micelles
Thenoyltrifluoroacetone (TTA)
  Mz+(aq) + zHTTA(org) <-->M(TTA)z(org) + H+(aq)
  What is the equilibrium constant?
Keto
Enol
Hydrate

## Slide 9: Extractant Ligands
α-hydroxyisobutyric acid
  Used in lanthanide separations
Di-(2-ethylhexyl) phosphoric acid (HDEHP)
  Exploited in solvent and solid systems
  TALSPEAK (Am)
HDEHP

## Slide 10: PUREX overview
PUREX (Pu-U Reduction EXtraction) liquid-liquid extraction process developed to recover Pu for weapons production
  Developed during Manhattan Project
    Patented 1947. deployment at Savannah River 1954 and Hanford 1956
  U and Pu extracted from aqueous to organic phase
  Pu reduced, goes to aqueous phase while U remains in organic phase
Decladding – mechanical, chemical
Nitric acid dissolution – e.g., rotary wheel
Solvent extraction and product preparation
  Includes purification step
Waste treatment and disposal – off-gases; acid, water, and solvent recycle

## Slide 11: PUREX Process
Irradiated uranium fuel dissolved in nitric acid
  contacted with a solution of TBP in kerosene
    30 % TBP in kerosene
Hexavalent and tetravalent ion extraction
UO22+(aq) + 2NO3-(aq) + 2TBP(org)  UO2(NO3)2(TBP)2 (org)
Pu4+(aq) + 4NO3-(aq) + 2TBP(org)  Pu(NO3)4(TBP)2 (org)
UO22+ and Pu4+ extracted in 3 M HNO3 to 6 M HNO3
  High Kd range for UO22+ and Pu4+
Metal ions with other oxidation states extract poorly
  Np oxidation state drives behavior in PUREX
    Np4+ and NpO22+ extracts over entire range
    NpO2+ begins to extract at high acid end of range
  Mono-, di-, and trivalent limited extraction
Reduction of Pu drives separation from U
  Trivalent Pu separates from hexavalent U by backextraction from organic

## Slide 12: PUREX Process
Pu reduction drives separation from U
  Trivalent Pu separates from hexavalent U by backextraction from organic
Pu reducing agents form Pu(III) which backextracts to aqueous phase
Ferrous sulfamate: Fe 2+: Fe(H2NO3S)2
  Pu 4+ + Fe 2+Pu 3+ + Fe 3+
Uranium (IV)
  2Pu 4+ + U 4+ + 2H2O  2Pu 3+ + UO2 2+ + 4 H+
Hydroxylamine nitrate (NH3OH+NO3-)

## Slide 13: Solvent Extraction in PUREX
Feed
Aqueous
Solution
U+Pu+ FP*
Solvent
Mixing
U+Pu+PF*
+
Solvent
PF*
Settling
U+Pu
+
Solvent
Centrifugal Contactor
Solvent
In
Moteur
Solvent Out
Loaded U + Pu
Exit
raffinate FP*
Protection
lead / concrete
Feed
Aqueous Phase
U+Pu+FP*
High Mixer
Settler
Pulsed Column
Feed
Aqueous Phase
U + Pu + FP*
Perforated
Plates
Exit
raffinate FP*
Low Mixer settler
Feed Solvent
Compressed Air
Interphase
Exit Solvent
Loaded U + Pu
* FP : Fission Products
PF*
Mixer settler
U+Pu+FP*
U+Pu
Solvent
Solvent
In
Feed
Aqueous Phase
U+Pu+FP*
Solvent
Out
Loaded with U+Pu
Exit
raffinate FP*

## Slide 14: PUREX process
Plant-scale performance of a two-cycle PUREX process:
  Separation of Pu from U: 106
  Separation of fission products from Pu: 108
  Separation of fission products from U: 107
  Pu and U recovery
How to achieve high separation with Kd on the order of 102
  Multiple stages
http://www.cresp.org/NuclearChemCourse/monographs/11_Law_Liquid-liquid%20extraction%20equipment%20jdl_3_2_09.pdf

## Slide 15: U-Pu separation in PUREX
Based on formation of nitrate species
  30 % TBP in kerosene
  3.5 M NHO3
  Strip has 0.1 M hydroxylamine nitrate in 3.5 M HNO3
Process example of pulse column below

## Slide 16: Third Phase Formation
In liquid-liquid solvent extraction certain conditions cause the organic phase to split
  PUREX separations TBP
  Possible with advanced separations
Limiting Organic Concentration (LOC) – highest metal content in phase prior to split
  Light phase – mostly diluent
  Heavy phase – extractant and metal rich
Safety issues, relate to criticality
Can be exploited for synthesis

## Slide 17: Actinide Third Phases
Light Phase
Heavy Phase
Aqueous
Phase
U(VI)
Pu(IV)
Np(IV)
Np(VI)
Pu(VI)

## Slide 19: RDCH 702: Lecture 9 Separations
Separation methods
  Solvent extraction
    PUREX
  Ion exchange
  Electrochemistry
  Volatility
Specific actinide separations
Basic concept of separations
  Oxidation state
  Ionic radius
Development of advanced separations
  Trivalent actinides
Necessary for fuel cycle due to formation of mixtures due to fission
  Actinides
    Transuranics
  Fission products
    Se (Z=34) to Dy (Z=66)
Tributyl phosphate (TBP)