## Slide 1: RDCH 702: Lecture 9 Separations Part 2
Separation methods
  Solvent extraction
    PUREX
  Ion exchange
  Volatility
  Electrochemistry
Specific actinide separations
Basic concept of separations
  Oxidation state
  Ionic radius
Development of advanced separations
  Trivalent actinides
Necessary for fuel cycle due to formation of mixtures due to fission
  Actinides
    Transuranics
  Fission products
    Se (Z=34) to Dy (Z=66)
Tributyl phosphate (TBP)

## Slide 2: Ion Exchange/Chromatography Separations
Dissolved sample, solid exchanger
Adjustment of solution matrix
  Based on column chemistry and other elements in solution
Retention of target radionuclide on column
  Removal of other elements
Solution adjustment
  Acid concentration, counter ion variation
  Addition of redox agent
Elute target radionuclide
Can include addition of isotopic tracer to determine yield
Chemical behavior measured by distribution
  Similar to Kd
    (mg metal/g resin)/(mg metal/mL solution)
    mL/g

## Slide 3: Ion Exchange Resins
Resins
  Organic or inorganic polymer used to exchange cations or anions from a solution phase
General Structure
  Polymer backbone not involved in bonding
  Functional group for complexing anion or cation
Properties
  Capacity
    Amount of exchangeable ions per unit quantity of material
      Proton exchange capacity (PEC), meq/g
  Selectivity
    Cation or anion exchange
      Cations are positive ions
      Anions are negative ions
    Some selectivities within group
      Distribution of metal ion can vary with solution

## Slide 4: Organic Resins
Backbone
  Cross linked polymer chain
    Divinylbenzene, polystyrene
    Cross linking limits swelling, restricts cavity size
Functional group
  Functionalize benzene
    Sulfonated to produce cation exchanger
    Chlorinated to produce anion exchanger
Structure
  Randomness in crosslinking produces disordered structure
    Range of distances between sites
    Environments
      Near organic backbone or mainly interacting with solution
Sorption based resins
Organic with long carbon chains (XAD resins)
  Sorbs organics from aqueous solutions
  Can be used to make functionalized exchangers
Cation exchange
Anion exchange
Linkage group

## Slide 5: Inorganic Resins
More formalized structures
  Less disorder
Silicates (SiO4)
Alumina (AlO4)
  Both tetrahedral
  Can be combined
    (Ca,Na)(Si4Al2O12).6H2O
  Aluminosilicates
    zeolite, montmorillonites
    Cation exchangers
    Can be synthesized
Zirconium, Tin- phosphate
  Easy to synthesis
    Metal salt with phosphate
    Precipitate forms
      Grind and sieve
  Zr can be replaced by other tetravalent metals
    Sn, Th, U
Zeolites
  Microporous, aluminosilicate minerals
  Used as sorbants

## Slide 6: Kinetics
Diffusion controlled
  Film diffusion
    On surface of resin
  Particle diffusion
    Movement into resin
Rate is generally fast
Increase in crosslinking decrease rate
Theoretical plates used to estimate reactions
Swelling
Solvation increases exchange
Greater swelling decreases selectivity
Sorption interactions of plutonium and europium with ordered mesoporous carbon

## Slide 7: Column Chromatography Ion Exchange
Chromatogram
  concentration versus elution time
Strongly retained species elutes last
  elution order
Analyte is diluted during elution
  dispersion
Zone broadening proportional to elution time
Separations enhanced by varying experimental conditions

## Slide 8: Broadening
Individual molecule undergoes "random walk"
Many thousands of adsorption/desorption processes
Average time for each step with some variations
  Gaussian peak
    like random errors
Breadth of band increases down column because more time
Efficient separations have minimal broadening

## Slide 9: Theoretical plates
Column efficiency increases with number of plates
  N=L/H
    N= number of plates, L = column length, H= plate height
  Assume equilibrium occurs at each plate
  Movement down column modeled
Plate number can be found experimentally
Other factors that impact efficiency
  Mobile Phase Velocity
  Higher mobile phase velocity
    less time on column
    less zone broadening

## Slide 10
    Kd = mL/g
    = (mg metal/g resin)/(mg metal/mL solution)

## Slide 12
Dv =([M]/mL resin)/([M]/mL solution)

## Slide 13: Volatility: AIROX
For treatment of oxide fuel
UO2 oxidized to U3O8
  Heating to 400-600 °C in O2 containing atmosphere
  Around 30% volume increase
U3O8 reduction by addition of H2
Kr, Xe, I removed
  Some discrepancies
Element | Ref. 1 | Ref. 2 | Ref. 3 | Ref. 4
Ag | 80 | 0 | 0 | 0
Cd | 0 | 75 | 75 | 80
Cs | 99 | 90 | 100 | 99
In | 0 | 75 | 0 | 75
Ir | 0 | 0 | 75 | 0
Mo | 80 | 0 | 0 | 80
Pd | 80 | 0 | 0 | 0
Rh | 80 | 0 | 0 | 0
Ru | 80 | 90 | 100 | 80
Se | 80 | 0 | 0 | 99
Tc | 80 | --- | 0 | 0
Te | 99 | 75 | 75 | 99
1. AECL Technologies, Inc. “Plutonium Consumption Program-CANDU Reactor Projects,” Final Report, July 1994.
2. SCIENTECH, Inc., Gamma Engineering Corp., “Conceptual Design and Cost Evaluation for the DUPIC Fuel Fabrication Facility,” Final Report, SCIE-COM-219-96, May 1996.
Recycling of Nuclear Spent Fuel with AIROX Processing, D. Majumdar Editor, DOE/ID-10423, December 1992.
Bollmann, C.A., Driscoll, M.J., and Kazimi, M.S.: Environmental and Economic Performance of Direct Use of PWR Spent Fuel in CANDU Reactors. MIT-NFC-TR-014, 44-45, June 1998.

## Slide 14: Element Volatility
Element | °C
He | -272
Kr | -157
Xe | -111
Cs | 29
Rb | 39
I | 114
Te | 450
Pu | 640
Ba | 725
Sr | 764
Ce | 795
Eu | 822
Element | °C
La | 920
Pr | 935
Nd | 1010
Pm | 1042
Sm | 1072
U | 1132
Y | 1523
Pd | 1552
Zr | 1852
Rh | 1966
Tc | 2200
Ru | 2250
Mo | 2617
Melting points correlate with vapor pressure
  Zone refining can have applications
Data for elements
  Need to consider solid solutions and intermetallics in fuel
Melting Points

## Slide 15: Volatility: CO2
Nearly 70 % of Eu, Gd, Nd, and Sm by oxidation under CO2 at 1000 °C
  Attributed to Rh as catalyst in matrix
  Volatile species not identified
Near complete removal for Ag, Cs, and Mo
Element | 750 °C | 1000 °C | 1250 °C
Cs | 7.84+0.96E-03 | 4.82±0.42E-02 | 1.72±0.59E-01
Ag | 1.09±0.22E-02 | 1.74±0.62E-01 | 5.25±0.38E-01
Rh | 9.22±0.40E-02 | 2.24±0.41E-01 | 4.94±0.54E-01
Eu | 3.28±0.34E-02 | 1.11±0.66E-01 | 2.84±0.29E-01
Sm | 3.85±0.54E-02 | 9.23±1.01E-02 | 2.15±0.29E-01
Nd | 3.99±0.94E-02 | 7.85±1.95E-02 | 1.96±0.20E-01
Evaluated rate constants (min-1) for the CO2 volatilization of Cs, Ag, Rh, Eu, Sm, and Nd in UO2

## Slide 16: Carbonyl (CO)
Metals form a range of complexes with CO
  Range of oxidation states
    0 to cations
Tends to form volatile species
Mond process
  Ni treated with CO at 60-80 °C
  Decomposes at 180 °C to form pure Ni and CO

## Slide 17: Carbonyl
No evidence of U or Pu carbonyl from direct reaction of CO with metal
Group 1 and 2
  Form true carbonyls with metals at very low temperature
No evidence of simple Zr carbonyls
  Laser ablation experiments
Lanthanides: Ln from laser ablation studies
  Volatile species observed
Noble metal: neutral binary carbonyls: Mo(CO)6, Tc, Ru, Rh
  Mo and Pd from the chloride
  Pd forms mixed halide carbonyl
  Ru(CO)5 volatile species at 25° has been observed
    Ru was on Al2O3 catalysts (mixed reactions)
Mo(CO)6

## Slide 18: Halides (F, Cl, Br, I)
Can be produced from direct metal reaction
  Compounds often unstable, mixed oxygen species common
Van Arkel process for obtaining pure Zr
  Zr with I2 at 200 °C forms ZrI4
  Zr tetrahalide critical temperatures (sublimation, triple point):
    F (600 °C), Cl (437 °C), Br (450 °C), I (499 °C)
metal is converted into a volatile halide compound
volatile compound is decomposed
  Can be used as plating method (i.e., Zr layer on metal fuel)

## Slide 19: Halides
Fluorination of simulated thermal reactor fuel containing UO2, PuO2, and fission product oxides has been studied
  U selectively fluorinated to UF6 with BrF5 at 200 to 400 oC.
  PuF4 converted to PuF6.
  Most fission products form fluorides that volatilize at high temperatures than the actinides
    Preferential distillation
Chlorination also examined, similar to fluoride behavior
Anatasia, L.J., Alfredson, P.G., and Steindler, M.J.: Fluidized-Bed Fluorination of UO2-PuO2-Fission Product Pellets with BrF5 and Fluorine. Part I: The Fluorination of Uranium, Neptunium, and Plutonium. Nuclear Applications and Technology, 7, 425-432, 1969.
Anatasia, L.J., Alfredson, P.G., and Steindler, M.J.: Fluidized-Bed Fluorination of UO2-PuO2-Fission Product Pellets with BrF5 and Fluorine. Part II: Process Considerations. Nuclear Applications and Technology, 7, 433-442, 1969.
Selvaduray, G., Goldstein, M.K., and Anderson, R.N.: Separation Technologies Reviewed. Nuclear Engineering International, 23, 35-40, 1978.

## Slide 20: Halides
Actinide halides
  Formed from other fluorides or dioxide in halide-organic solvents
    2AlCl3 + UF6 2AlF3 + UCl6
    UF4 can be prepared from UO2 + NH4HF2
    Heating metal with I2 can form AnI3
  Melting points
    AnF6: U= 64 °C, Np=55 °C, Pu = 52 °C
    AnF4: U=1036 °C, Pu= 1027 °C
    UCl6 (177 °C)
    AnCl4: U = 590 °C, Np = 517 °C
    AnI3: U=766 °C, Np = 760 °C, Pu = 777 °C
→

## Slide 21: Halides
Group 1
  Produced from the carbonate or hydroxide and HX (halide acid)
  Can be made by metal reaction
  Melting points
    Trends: F>Cl>Br>I
      Rb: 642 °C to 823 °C; Cs: 621 °C to 703 °C
Group 2
  Can be formed from direct metal reaction
  Trend as Group 1
  melting points (538 °C [SrI2] to 1477 °C [SrF2]
Lanthanides
  Metal reactions
  Melting point
    Over 1200 °C for fluorides, 600 °C to 800 °C for other halides

## Slide 22: Halides: Example with Tc
Direct reaction of the elements:
6 hours
T = 400 ºC
Br2
I2
Before
6 hours
T = 400 ºC
Br2
I2
After
Formation of volatile Tc-Br species

## Slide 23: Hexafluoroacetylacetonate (hfac)
Complexes known for high volatility and ease of synthesis
Can be used to effect separation directly from a mixture of metal oxides with solvent free reactions
  Solvent free: mixing of solids
U from Pb demonstrated in solvent
  Selective species formation
hfac used for vapor deposition of metal
  Possible route to separation and metal formation in single step
Initial studies performed with actinides, lanthanides and fission elements

## Slide 24: RDCH 702: Lecture 9 Separations Part 2
Separation methods
  Solvent extraction
    PUREX
  Ion exchange
  Volatility
  Electrochemistry
Specific actinide separations
Basic concept of separations
  Oxidation state
  Ionic radius
Development of advanced separations
  Trivalent actinides
Necessary for fuel cycle due to formation of mixtures due to fission
  Actinides
    Transuranics
  Fission products
    Se (Z=34) to Dy (Z=66)
Tributyl phosphate (TBP)