## Slide 1: RDCH 702: Lecture 9 Separations Part 3
Separation methods
  Solvent extraction
    PUREX
  Ion exchange
  Volatility
  Electrochemistry
Specific actinide separations
Basic concept of separations
  Oxidation state
  Ionic radius
Development of advanced separations
  Trivalent actinides
Necessary for fuel cycle due to formation of mixtures due to fission
  Actinides
    Transuranics
  Fission products
    Se (Z=34) to Dy (Z=66)
Tributyl phosphate (TBP)

## Slide 2: Pyroprocesses
Electrorefining/Electrochemistry
Uses molten salt as solvent
  KCl-NaCl
  Avoids problems associated with aqueous chemistry
    Hydrolysis and chemical instability
Reduction of metal ions to metallic state
Differences in free energy between metal ions and salt
Thermodynamic data at hand or easy to obtain
Sequential oxidation/reduction
  Cations transported through salt and deposited on cathode
  Deposition of ions depends upon redox potential

## Slide 3: Electrochemical Separations
Selection of redox potential allows separations
  Can use variety of electrodes for separation
Free energies
  noble metals
  iron to zirconium
  actinides and rare earths
  Group 1 and 2
Solubility of chlorides in cadmium
Explored at part of Integral Fast Reactor (IFR) program

## Slide 4: Molten Salt
Volatility of chlorides as separation basis
  Gaps between groups
  High vapor pressures achievable at low temperature

## Slide 5: Molten Salt Example
Oxide fuel dispersed in CaCl2 /CaF2 at 800 °C
  Inclusion of Ca metal reduces U salt to a metal
Reduced metals dissolved in receiver alloy
  Example Cu - 40% Mg - Ca
  Uranium exceeds solubility limits receiver alloy and precipitates
Pu, other actinides, rare-earths, and noble metal fission products accumulate in receiver alloy
  Separated by distillation
Alkali metals (Rb and Cs), alkali-earths (Sr and Ba),and remaining iodine and bromine accumulate in the CaCl2/CaF2 salt.
Salt contains CaO from the reduction process
  CaO is electrolytically reduced to metal for reuse

## Slide 6: Molten Salt
LiCl-KCl-UCl3 at 450-500 oC
Chopped metallic fuel added to anode baskets
  U oxidized at anode to U(III)
  Reduced back to metal at cathode
Transuranics and fission products oxidized
  Co-deposition of actinides with cadmium cathode

## Slide 7: Pu Processing
DOR reduces plutonium dioxide to metal
  PuO2 and Ca/CaCl2
  Formation of Pu metal and CaO
  CaO treated with Cl2
Pu metal purified by electrorefining
Pu metal melted in NaCl/KCl at 800°C
Pu oxidized to PuCl3,
  dissolves in molten salt
PuCl3 migrates to cathode and reduced
Pu metal drips from cathode and collects in annular region outside cup
  ring of pure Pu produced

## Slide 8: Ionic liquids
Room temperature ionic liquid (ILs) composed of ions that are liquid below 373 K
Composed of a bulky, unsymmetrical organic cation and an organic or inorganic anion
  Range of possible pairs, can be task specific
    Low vapor pressure
    Ability to dissolve organic and inorganic compounds
    Conductive
    Wide electrochemical window
Ionic liquids are tunable to obtain properties needed for particular application
  Solubility
  Reaction Rate
  Electrochemical window
  Specific metal ion interaction

## Slide 9: Introduction: Ionic liquids
Ethylammonium nitrate electrochemistry in 1914
Initial efforts focused on chloroaluminate anion (AlCl4-)
  Electroplate aluminum
    J. Electrochem. Soc. 98, 203 (1951)
  Detailed studies, identification of limitations with chloroaluminate
    Moisture sensitivity
    Requires non-ambient conditions
      Inorg. Chem. 17, 2728 (1978)
Newer ionic liquids have non-hydrolyzing or stable anions
  Moisture stable ionic liquids developed
    JACS, 965 (1992)

## Slide 10: Examples of IL cations and anions
1018 possible combinations
Route for task specific properties
  Group actinide separation
Can functionalize ILs

## Slide 11: Ionic liquids in separations
Ionic liquids can replace traditional solvents in the PUREX
  Studies showed favorable extraction when ILs used in conjunction with extractants
  Chem. Commun. 1765 (1998)
Possible recovery of metals through electrodeposition
  direct from the organic phase following solvent extraction
  From J. Nucl. Radiochem. Sci., 10(1), 1-6 (2009)

## Slide 12: f-element reduction in ionic liquids
Haloaluminates not stable to reduction of An(III) or Ln(III) to metal state
Development of moisture-stable ILs
  good cathodic stability
  large ~6V electrochemical windows
Application based upon the molten salt system (450 - 800°C)
  Ionic liquids eliminate
    Specialized corrosion resistant cell
    Operation at elevated temperatures
    Production of caustic side reactions
Electrochemistry of Sm3+, La3+, Eu3+ and Th4+ in [Me3NBu][TFSI]
  Reported reduction of Sm, La, and Eu to the metallic state
  Th was reported to reduce to Th0 but subsequently was converted to ThO2 by moisture in ionic liquid
    Dalton Trans, 24, 4532-4534 (2002)
Role of water central, useful in dissolution by problematic in full reduction

## Slide 13: Choice of Ionic Liquid
A number of ionic liquids initially investigated
bis(trifluoromethanesulfonyl)imide (TFSI) anion selected for study at UNLV
  Functionalized TFSI evaluated
    propyl and imidazolium
  large potential window with Au, Pt, and Glassy carbon electrodes
    Suitable for reduction of lanthanides and actinides
Ionic liquid
  N-trimethyl-N-butylammonium bis(trifluoromethanesulfonyl)imide
    Used with actinides
  Written as [Me3NBu][TFSI]

## Slide 14: Electrochemistry in ionic liquids
ILs have wider potential window
  Actinide electrochemistry possible
  Must limit water in the system
TFSI is a poor ligand
  Moves deposition to favorable potential
Electrode can influence window
  Glassy Carbon (GC) widest potential window

## Slide 15: U TFSI compound synthesis
All reactions were performed in an argon filled glove box
K(TFSI)(s) synthesized by adding H(TFSI) and KH THF solution
  K(TFSI) separated by decanting excess THF
    90% yield
K(TFSI) and UI3(THF)4 dissolved in THF
  Excess of K(TFSI) added to ensure reaction completion
  Clear pale yellow solution was stirred for 24 hours
  Final orange red solution
    Contained off white KI solid precipitate
    THF solution contained product U(TFSI)3
    Solid was isolated by evaporating excess THF
      74% yield

## Slide 16: Formation of Uranium Deposits
Constant potential of -1.5 V versus NHE
SEM, EDS, and XRD analysis performed
SEM of U deposited on Au foil
XRD evaluation of sample
  Alpha U metal
SEM EDS
  No oxygen at 5.5 keV
Au electrode
U-metal deposit

## Slide 17: Direct dissolution of U3O8 into ionic liquid
Original dissolution conditions:
45 mg U3O8 with 3.27 M HTFSI in Me3NBuTFSI Stirred for weeks with no change
RESULT: dissolution of material
oxidizing gas used
  O3, NO2
Addition of HTFSI
  Promote formation of uranium-TFSI complex
Ozone
(From compressed air)
t = 24 hrs

## Slide 18: Direct dissolution of U3O8 into RTIL
Proposed dissolution mechanism:
U3O8 + 6 HTFSI + O3 3 UO22+ + 6 TFSI- + 3 H2O + O2
Supporting EXAFS data of the original dissolution solution
confirmed presence of UO22+
coordinated with five to six equatorial oxygens.
2 O @ 1.75 Å
6 ± 1 O @ 2.38 Å
U --- O multi scattering @ 3.56 Å

## Slide 19: RDCH 702: Lecture 9 Separations Part 3
Separation methods
  Solvent extraction
    PUREX
  Ion exchange
  Volatility
  Electrochemistry
Specific actinide separations
Basic concept of separations
  Oxidation state
  Ionic radius
Development of advanced separations
  Trivalent actinides
Necessary for fuel cycle due to formation of mixtures due to fission
  Actinides
    Transuranics
  Fission products
    Se (Z=34) to Dy (Z=66)
Tributyl phosphate (TBP)