## Slide 1: RDCH 702: Lecture 9 Separations
Separation methods
  Solvent extraction
    PUREX
  Ion exchange
  Volatility
  Electrochemistry
Specific actinide separations
Basic concept of separations
  Oxidation state
  Ionic radius
Development of advanced separations
  Trivalent actinides
Necessary for fuel cycle due to formation of mixtures due to fission
  Actinides
    Transuranics
  Fission products
    Se (Z=34) to Dy (Z=66)
Tributyl phosphate (TBP)

## Slide 2: Solvent Extraction
Two phase system for separation
  Sample dissolved in aqueous phase
    Normally acidic phase
Aqueous phase contacted with organic containing ligand
  Formation of neutral metal-ligand species drives solubility in organic phase
Organic phase contains target radionuclide
  May have other metal ions, further separation needed
    Variation of redox state, contact with different aqueous phase
Back extraction of target radionuclide into aqueous phase
  Reduction of Pu to trivalent
Distribution between organic and aqueous phase measured to evaluate chemical behavior

## Slide 3: Solvent extraction
Influence of chemical conditions
  Solvent
  Metal ion and acid concentration
    Phase splitting
Distribution coefficient
  Used to determine separation factors for a given metal ion
    Ratio of Kd for different metal ions
      May be represented by Kd or D
    Kd= 1
      50 % of metal in organic phase
    Kd= 10
      90.9 % of metal in organic phase
    Kd= 100
      99.01 % of metal in organic phase
  Distribution can be used to evaluate stoichiometry
    Evaluation distribution against change in solution parameter
      Plot log Kd versus log [X], slope is stoichiometry
Extraction can be explained by complexation
  Used to determine complexation constants

## Slide 4: Distribution coefficient and stoichiometry
Plot log Kd versus log [X]
  slope is stoichiometry of evaluated parameter
Consider reaction
  xM + yLMxLy
    Want to determine value for y
    Plot log Kd against log [L]
Use complexation constant and distribution coefficient
,
Substitute Kd into K equation, x=1
Log of equation
  Log K = log Kd – y log [L]; rearrange equation
  Log Kd = Log K + y log [L]
    Log K is constant
    Slope of log Kd versus log L gives y, the L stoichiometry

## Slide 5
Oxidation state importance
D variation with acid concentration

## Slide 6: Solvation Extraction Mechanism
CMPO
Extraction of neutral complex
  UO2(NO3)2 forms with TBP (P=O functional group)
    Equilibrium shifts with nitrate, back extraction into aqueous at low nitric acid
Other extractants include bifunctional ligands
  Carbamoyl phosphate compounds
    2 to 4 CMP per extracted molecule
  Carbamoylphosphine oxide (CMPO)
    2 CMPO for U and Pu, 3 for trivalents
      Basis of TRUEX separation for Ln/An
  Malonamide extracts can replace CMPO
    CHON principle
    DIAMEX process
Malonamide

## Slide 7: Ion Pair Formation
Charged metal complex with extractant of opposite charge
  Quaternary ammonium salt with anionic actinide nitrate
    R4N+
    Aliquat 336
  Tertiary amines
    R3HN+AnXn-(n-z) for monovalent X with An with Z charge
      Require equilibration with acid
Can be sorbed to resins for separations
  TEVA resins

## Slide 8: Liquid cation exchanger and chelating agents
Metal ion exchanged into organic phase, ion transfer in aqueous phase
Use of organic soluble acid
  i.e., alkyl phosphinic acid (R2PO2H)
Can be controlled by acidity
May form aggregates or micelles
Thenoyltrifluoroacetone (TTA)
  Mz+(aq) + zHTTA(org) <-->M(TTA)z(org) + H+(aq)
  What is the equilibrium constant?
Keto
Enol
Hydrate

## Slide 9: Extractant Ligands
α-hydroxyisobutyric acid
  Used in lanthanide separations
Di-(2-ethylhexyl) phosphoric acid (HDEHP)
  Exploited in solvent and solid systems
  TALSPEAK (Am)
HDEHP

## Slide 10: PUREX overview
PUREX (Pu-U Reduction EXtraction) liquid-liquid extraction process developed to recover Pu for weapons production
  Developed during Manhattan Project
    Patented 1947. deployment at Savannah River 1954 and Hanford 1956
  U and Pu extracted from aqueous to organic phase
  Pu reduced, goes to aqueous phase while U remains in organic phase
Decladding – mechanical, chemical
Nitric acid dissolution – e.g., rotary wheel
Solvent extraction and product preparation
  Includes purification step
Waste treatment and disposal – off-gases; acid, water, and solvent recycle

## Slide 11: PUREX Process
Irradiated uranium fuel dissolved in nitric acid
  contacted with a solution of TBP in kerosene
    30 % TBP in kerosene
Hexavalent and tetravalent ion extraction
UO22+(aq) + 2NO3-(aq) + 2TBP(org)  UO2(NO3)2(TBP)2 (org)
Pu4+(aq) + 4NO3-(aq) + 2TBP(org)  Pu(NO3)4(TBP)2 (org)
UO22+ and Pu4+ extracted in 3 M HNO3 to 6 M HNO3
  High Kd range for UO22+ and Pu4+
Metal ions with other oxidation states extract poorly
  Np oxidation state drives behavior in PUREX
    Np4+ and NpO22+ extracts over entire range
    NpO2+ begins to extract at high acid end of range
  Mono-, di-, and trivalent limited extraction
Reduction of Pu drives separation from U
  Trivalent Pu separates from hexavalent U by backextraction from organic

## Slide 12: PUREX Process
Pu reduction drives separation from U
  Trivalent Pu separates from hexavalent U by backextraction from organic
Pu reducing agents form Pu(III) which backextracts to aqueous phase
Ferrous sulfamate: Fe 2+: Fe(H2NO3S)2
  Pu 4+ + Fe 2+Pu 3+ + Fe 3+
Uranium (IV)
  2Pu 4+ + U 4+ + 2H2O  2Pu 3+ + UO2 2+ + 4 H+
Hydroxylamine nitrate (NH3OH+NO3-)

## Slide 13: Solvent Extraction in PUREX
Feed
Aqueous
Solution
U+Pu+ FP*
Solvent
Mixing
U+Pu+PF*
+
Solvent
PF*
Settling
U+Pu
+
Solvent
Centrifugal Contactor
Solvent
In
Moteur
Solvent Out
Loaded U + Pu
Exit
raffinate FP*
Protection
lead / concrete
Feed
Aqueous Phase
U+Pu+FP*
High Mixer
Settler
Pulsed Column
Feed
Aqueous Phase
U + Pu + FP*
Perforated
Plates
Exit
raffinate FP*
Low Mixer settler
Feed Solvent
Compressed Air
Interphase
Exit Solvent
Loaded U + Pu
* FP : Fission Products
PF*
Mixer settler
U+Pu+FP*
U+Pu
Solvent
Solvent
In
Feed
Aqueous Phase
U+Pu+FP*
Solvent
Out
Loaded with U+Pu
Exit
raffinate FP*

## Slide 14: PUREX process
Plant-scale performance of a two-cycle PUREX process:
  Separation of Pu from U: 106
  Separation of fission products from Pu: 108
  Separation of fission products from U: 107
  Pu and U recovery
How to achieve high separation with Kd on the order of 102
  Multiple stages
http://www.cresp.org/NuclearChemCourse/monographs/11_Law_Liquid-liquid%20extraction%20equipment%20jdl_3_2_09.pdf

## Slide 15: U-Pu separation in PUREX
Based on formation of nitrate species
  30 % TBP in kerosene
  3.5 M NHO3
  Strip has 0.1 M hydroxylamine nitrate in 3.5 M HNO3
Process example of pulse column below

## Slide 16: Third Phase Formation
In liquid-liquid solvent extraction certain conditions cause the organic phase to split
  PUREX separations TBP
  Possible with advanced separations
Limiting Organic Concentration (LOC) – highest metal content in phase prior to split
  Light phase – mostly diluent
  Heavy phase – extractant and metal rich
Safety issues, relate to criticality
Can be exploited for synthesis

## Slide 17: Actinide Third Phases
Light Phase
Heavy Phase
Aqueous
Phase
U(VI)
Pu(IV)
Np(IV)
Np(VI)
Pu(VI)

## Slide 19: RDCH 702: Lecture 9 Separations
Separation methods
  Solvent extraction
    PUREX
  Ion exchange
  Volatility
  Electrochemistry
Specific actinide separations
Basic concept of separations
  Oxidation state
  Ionic radius
Development of advanced separations
  Trivalent actinides
Necessary for fuel cycle due to formation of mixtures due to fission
  Actinides
    Transuranics
  Fission products
    Se (Z=34) to Dy (Z=66)
Tributyl phosphate (TBP)

## Slide 20: RDCH 702: Lecture 9 Separations Part 2
Separation methods
  Solvent extraction
    PUREX
  Ion exchange
  Volatility
  Electrochemistry
Specific actinide separations
Basic concept of separations
  Oxidation state
  Ionic radius
Development of advanced separations
  Trivalent actinides
Necessary for fuel cycle due to formation of mixtures due to fission
  Actinides
    Transuranics
  Fission products
    Se (Z=34) to Dy (Z=66)
Tributyl phosphate (TBP)

## Slide 21: Ion Exchange/Chromatography Separations
Dissolved sample, solid exchanger
Adjustment of solution matrix
  Based on column chemistry and other elements in solution
Retention of target radionuclide on column
  Removal of other elements
Solution adjustment
  Acid concentration, counter ion variation
  Addition of redox agent
Elute target radionuclide
Can include addition of isotopic tracer to determine yield
Chemical behavior measured by distribution
  Similar to Kd
    (mg metal/g resin)/(mg metal/mL solution)
    mL/g

## Slide 22: Ion Exchange Resins
Resins
  Organic or inorganic polymer used to exchange cations or anions from a solution phase
General Structure
  Polymer backbone not involved in bonding
  Functional group for complexing anion or cation
Properties
  Capacity
    Amount of exchangeable ions per unit quantity of material
      Proton exchange capacity (PEC), meq/g
  Selectivity
    Cation or anion exchange
      Cations are positive ions
      Anions are negative ions
    Some selectivities within group
      Distribution of metal ion can vary with solution

## Slide 23: Organic Resins
Backbone
  Cross linked polymer chain
    Divinylbenzene, polystyrene
    Cross linking limits swelling, restricts cavity size
Functional group
  Functionalize benzene
    Sulfonated to produce cation exchanger
    Chlorinated to produce anion exchanger
Structure
  Randomness in crosslinking produces disordered structure
    Range of distances between sites
    Environments
      Near organic backbone or mainly interacting with solution
Sorption based resins
Organic with long carbon chains (XAD resins)
  Sorbs organics from aqueous solutions
  Can be used to make functionalized exchangers
Cation exchange
Anion exchange
Linkage group

## Slide 24: Inorganic Resins
More formalized structures
  Less disorder
Silicates (SiO4)
Alumina (AlO4)
  Both tetrahedral
  Can be combined
    (Ca,Na)(Si4Al2O12).6H2O
  Aluminosilicates
    zeolite, montmorillonites
    Cation exchangers
    Can be synthesized
Zirconium, Tin- phosphate
  Easy to synthesis
    Metal salt with phosphate
    Precipitate forms
      Grind and sieve
  Zr can be replaced by other tetravalent metals
    Sn, Th, U
Zeolites
  Microporous, aluminosilicate minerals
  Used as sorbants

## Slide 25: Kinetics
Diffusion controlled
  Film diffusion
    On surface of resin
  Particle diffusion
    Movement into resin
Rate is generally fast
Increase in crosslinking decrease rate
Theoretical plates used to estimate reactions
Swelling
Solvation increases exchange
Greater swelling decreases selectivity
Sorption interactions of plutonium and europium with ordered mesoporous carbon

## Slide 26: Column Chromatography Ion Exchange
Chromatogram
  concentration versus elution time
Strongly retained species elutes last
  elution order
Analyte is diluted during elution
  dispersion
Zone broadening proportional to elution time
Separations enhanced by varying experimental conditions

## Slide 27: Broadening
Individual molecule undergoes "random walk"
Many thousands of adsorption/desorption processes
Average time for each step with some variations
  Gaussian peak
    like random errors
Breadth of band increases down column because more time
Efficient separations have minimal broadening

## Slide 28: Theoretical plates
Column efficiency increases with number of plates
  N=L/H
    N= number of plates, L = column length, H= plate height
  Assume equilibrium occurs at each plate
  Movement down column modeled
Plate number can be found experimentally
Other factors that impact efficiency
  Mobile Phase Velocity
  Higher mobile phase velocity
    less time on column
    less zone broadening

## Slide 29
    Kd = mL/g
    = (mg metal/g resin)/(mg metal/mL solution)

## Slide 31
Dv =([M]/mL resin)/([M]/mL solution)

## Slide 32: Volatility: AIROX
For treatment of oxide fuel
UO2 oxidized to U3O8
  Heating to 400-600 °C in O2 containing atmosphere
  Around 30% volume increase
U3O8 reduction by addition of H2
Kr, Xe, I removed
  Some discrepancies
Element | Ref. 1 | Ref. 2 | Ref. 3 | Ref. 4
Ag | 80 | 0 | 0 | 0
Cd | 0 | 75 | 75 | 80
Cs | 99 | 90 | 100 | 99
In | 0 | 75 | 0 | 75
Ir | 0 | 0 | 75 | 0
Mo | 80 | 0 | 0 | 80
Pd | 80 | 0 | 0 | 0
Rh | 80 | 0 | 0 | 0
Ru | 80 | 90 | 100 | 80
Se | 80 | 0 | 0 | 99
Tc | 80 | --- | 0 | 0
Te | 99 | 75 | 75 | 99
1. AECL Technologies, Inc. “Plutonium Consumption Program-CANDU Reactor Projects,” Final Report, July 1994.
2. SCIENTECH, Inc., Gamma Engineering Corp., “Conceptual Design and Cost Evaluation for the DUPIC Fuel Fabrication Facility,” Final Report, SCIE-COM-219-96, May 1996.
Recycling of Nuclear Spent Fuel with AIROX Processing, D. Majumdar Editor, DOE/ID-10423, December 1992.
Bollmann, C.A., Driscoll, M.J., and Kazimi, M.S.: Environmental and Economic Performance of Direct Use of PWR Spent Fuel in CANDU Reactors. MIT-NFC-TR-014, 44-45, June 1998.

## Slide 33: Element Volatility
Element | °C
He | -272
Kr | -157
Xe | -111
Cs | 29
Rb | 39
I | 114
Te | 450
Pu | 640
Ba | 725
Sr | 764
Ce | 795
Eu | 822
Element | °C
La | 920
Pr | 935
Nd | 1010
Pm | 1042
Sm | 1072
U | 1132
Y | 1523
Pd | 1552
Zr | 1852
Rh | 1966
Tc | 2200
Ru | 2250
Mo | 2617
Melting points correlate with vapor pressure
  Zone refining can have applications
Data for elements
  Need to consider solid solutions and intermetallics in fuel
Melting Points

## Slide 34: Volatility: CO2
Nearly 70 % of Eu, Gd, Nd, and Sm by oxidation under CO2 at 1000 °C
  Attributed to Rh as catalyst in matrix
  Volatile species not identified
Near complete removal for Ag, Cs, and Mo
Element | 750 °C | 1000 °C | 1250 °C
Cs | 7.84+0.96E-03 | 4.82±0.42E-02 | 1.72±0.59E-01
Ag | 1.09±0.22E-02 | 1.74±0.62E-01 | 5.25±0.38E-01
Rh | 9.22±0.40E-02 | 2.24±0.41E-01 | 4.94±0.54E-01
Eu | 3.28±0.34E-02 | 1.11±0.66E-01 | 2.84±0.29E-01
Sm | 3.85±0.54E-02 | 9.23±1.01E-02 | 2.15±0.29E-01
Nd | 3.99±0.94E-02 | 7.85±1.95E-02 | 1.96±0.20E-01
Evaluated rate constants (min-1) for the CO2 volatilization of Cs, Ag, Rh, Eu, Sm, and Nd in UO2

## Slide 35: Carbonyl (CO)
Metals form a range of complexes with CO
  Range of oxidation states
    0 to cations
Tends to form volatile species
Mond process
  Ni treated with CO at 60-80 °C
  Decomposes at 180 °C to form pure Ni and CO

## Slide 36: Carbonyl
No evidence of U or Pu carbonyl from direct reaction of CO with metal
Group 1 and 2
  Form true carbonyls with metals at very low temperature
No evidence of simple Zr carbonyls
  Laser ablation experiments
Lanthanides: Ln from laser ablation studies
  Volatile species observed
Noble metal: neutral binary carbonyls: Mo(CO)6, Tc, Ru, Rh
  Mo and Pd from the chloride
  Pd forms mixed halide carbonyl
  Ru(CO)5 volatile species at 25° has been observed
    Ru was on Al2O3 catalysts (mixed reactions)
Mo(CO)6

## Slide 37: Halides (F, Cl, Br, I)
Can be produced from direct metal reaction
  Compounds often unstable, mixed oxygen species common
Van Arkel process for obtaining pure Zr
  Zr with I2 at 200 °C forms ZrI4
  Zr tetrahalide critical temperatures (sublimation, triple point):
    F (600 °C), Cl (437 °C), Br (450 °C), I (499 °C)
metal is converted into a volatile halide compound
volatile compound is decomposed
  Can be used as plating method (i.e., Zr layer on metal fuel)

## Slide 38: Halides
Fluorination of simulated thermal reactor fuel containing UO2, PuO2, and fission product oxides has been studied
  U selectively fluorinated to UF6 with BrF5 at 200 to 400 oC.
  PuF4 converted to PuF6.
  Most fission products form fluorides that volatilize at high temperatures than the actinides
    Preferential distillation
Chlorination also examined, similar to fluoride behavior
Anatasia, L.J., Alfredson, P.G., and Steindler, M.J.: Fluidized-Bed Fluorination of UO2-PuO2-Fission Product Pellets with BrF5 and Fluorine. Part I: The Fluorination of Uranium, Neptunium, and Plutonium. Nuclear Applications and Technology, 7, 425-432, 1969.
Anatasia, L.J., Alfredson, P.G., and Steindler, M.J.: Fluidized-Bed Fluorination of UO2-PuO2-Fission Product Pellets with BrF5 and Fluorine. Part II: Process Considerations. Nuclear Applications and Technology, 7, 433-442, 1969.
Selvaduray, G., Goldstein, M.K., and Anderson, R.N.: Separation Technologies Reviewed. Nuclear Engineering International, 23, 35-40, 1978.

## Slide 39: Halides
Actinide halides
  Formed from other fluorides or dioxide in halide-organic solvents
    2AlCl3 + UF6 2AlF3 + UCl6
    UF4 can be prepared from UO2 + NH4HF2
    Heating metal with I2 can form AnI3
  Melting points
    AnF6: U= 64 °C, Np=55 °C, Pu = 52 °C
    AnF4: U=1036 °C, Pu= 1027 °C
    UCl6 (177 °C)
    AnCl4: U = 590 °C, Np = 517 °C
    AnI3: U=766 °C, Np = 760 °C, Pu = 777 °C
→

## Slide 40: Halides
Group 1
  Produced from the carbonate or hydroxide and HX (halide acid)
  Can be made by metal reaction
  Melting points
    Trends: F>Cl>Br>I
      Rb: 642 °C to 823 °C; Cs: 621 °C to 703 °C
Group 2
  Can be formed from direct metal reaction
  Trend as Group 1
  melting points (538 °C [SrI2] to 1477 °C [SrF2]
Lanthanides
  Metal reactions
  Melting point
    Over 1200 °C for fluorides, 600 °C to 800 °C for other halides

## Slide 41: Halides: Example with Tc
Direct reaction of the elements:
6 hours
T = 400 ºC
Br2
I2
Before
6 hours
T = 400 ºC
Br2
I2
After
Formation of volatile Tc-Br species

## Slide 42: Hexafluoroacetylacetonate (hfac)
Complexes known for high volatility and ease of synthesis
Can be used to effect separation directly from a mixture of metal oxides with solvent free reactions
  Solvent free: mixing of solids
U from Pb demonstrated in solvent
  Selective species formation
hfac used for vapor deposition of metal
  Possible route to separation and metal formation in single step
Initial studies performed with actinides, lanthanides and fission elements

## Slide 43: RDCH 702: Lecture 9 Separations Part 2
Separation methods
  Solvent extraction
    PUREX
  Ion exchange
  Volatility
  Electrochemistry
Specific actinide separations
Basic concept of separations
  Oxidation state
  Ionic radius
Development of advanced separations
  Trivalent actinides
Necessary for fuel cycle due to formation of mixtures due to fission
  Actinides
    Transuranics
  Fission products
    Se (Z=34) to Dy (Z=66)
Tributyl phosphate (TBP)

## Slide 44: RDCH 702: Lecture 9 Separations Part 3
Separation methods
  Solvent extraction
    PUREX
  Ion exchange
  Volatility
  Electrochemistry
Specific actinide separations
Basic concept of separations
  Oxidation state
  Ionic radius
Development of advanced separations
  Trivalent actinides
Necessary for fuel cycle due to formation of mixtures due to fission
  Actinides
    Transuranics
  Fission products
    Se (Z=34) to Dy (Z=66)
Tributyl phosphate (TBP)

## Slide 45: Pyroprocesses
Electrorefining/Electrochemistry
Uses molten salt as solvent
  KCl-NaCl
  Avoids problems associated with aqueous chemistry
    Hydrolysis and chemical instability
Reduction of metal ions to metallic state
Differences in free energy between metal ions and salt
Thermodynamic data at hand or easy to obtain
Sequential oxidation/reduction
  Cations transported through salt and deposited on cathode
  Deposition of ions depends upon redox potential

## Slide 46: Electrochemical Separations
Selection of redox potential allows separations
  Can use variety of electrodes for separation
Free energies
  noble metals
  iron to zirconium
  actinides and rare earths
  Group 1 and 2
Solubility of chlorides in cadmium
Explored at part of Integral Fast Reactor (IFR) program

## Slide 47: Molten Salt
Volatility of chlorides as separation basis
  Gaps between groups
  High vapor pressures achievable at low temperature

## Slide 48: Molten Salt Example
Oxide fuel dispersed in CaCl2 /CaF2 at 800 °C
  Inclusion of Ca metal reduces U salt to a metal
Reduced metals dissolved in receiver alloy
  Example Cu - 40% Mg - Ca
  Uranium exceeds solubility limits receiver alloy and precipitates
Pu, other actinides, rare-earths, and noble metal fission products accumulate in receiver alloy
  Separated by distillation
Alkali metals (Rb and Cs), alkali-earths (Sr and Ba),and remaining iodine and bromine accumulate in the CaCl2/CaF2 salt.
Salt contains CaO from the reduction process
  CaO is electrolytically reduced to metal for reuse

## Slide 49: Molten Salt
LiCl-KCl-UCl3 at 450-500 oC
Chopped metallic fuel added to anode baskets
  U oxidized at anode to U(III)
  Reduced back to metal at cathode
Transuranics and fission products oxidized
  Co-deposition of actinides with cadmium cathode

## Slide 50: Pu Processing
DOR reduces plutonium dioxide to metal
  PuO2 and Ca/CaCl2
  Formation of Pu metal and CaO
  CaO treated with Cl2
Pu metal purified by electrorefining
Pu metal melted in NaCl/KCl at 800°C
Pu oxidized to PuCl3,
  dissolves in molten salt
PuCl3 migrates to cathode and reduced
Pu metal drips from cathode and collects in annular region outside cup
  ring of pure Pu produced

## Slide 51: Ionic liquids
Room temperature ionic liquid (ILs) composed of ions that are liquid below 373 K
Composed of a bulky, unsymmetrical organic cation and an organic or inorganic anion
  Range of possible pairs, can be task specific
    Low vapor pressure
    Ability to dissolve organic and inorganic compounds
    Conductive
    Wide electrochemical window
Ionic liquids are tunable to obtain properties needed for particular application
  Solubility
  Reaction Rate
  Electrochemical window
  Specific metal ion interaction

## Slide 52: Introduction: Ionic liquids
Ethylammonium nitrate electrochemistry in 1914
Initial efforts focused on chloroaluminate anion (AlCl4-)
  Electroplate aluminum
    J. Electrochem. Soc. 98, 203 (1951)
  Detailed studies, identification of limitations with chloroaluminate
    Moisture sensitivity
    Requires non-ambient conditions
      Inorg. Chem. 17, 2728 (1978)
Newer ionic liquids have non-hydrolyzing or stable anions
  Moisture stable ionic liquids developed
    JACS, 965 (1992)

## Slide 53: Examples of IL cations and anions
1018 possible combinations
Route for task specific properties
  Group actinide separation
Can functionalize ILs

## Slide 54: Ionic liquids in separations
Ionic liquids can replace traditional solvents in the PUREX
  Studies showed favorable extraction when ILs used in conjunction with extractants
  Chem. Commun. 1765 (1998)
Possible recovery of metals through electrodeposition
  direct from the organic phase following solvent extraction
  From J. Nucl. Radiochem. Sci., 10(1), 1-6 (2009)

## Slide 55: f-element reduction in ionic liquids
Haloaluminates not stable to reduction of An(III) or Ln(III) to metal state
Development of moisture-stable ILs
  good cathodic stability
  large ~6V electrochemical windows
Application based upon the molten salt system (450 - 800°C)
  Ionic liquids eliminate
    Specialized corrosion resistant cell
    Operation at elevated temperatures
    Production of caustic side reactions
Electrochemistry of Sm3+, La3+, Eu3+ and Th4+ in [Me3NBu][TFSI]
  Reported reduction of Sm, La, and Eu to the metallic state
  Th was reported to reduce to Th0 but subsequently was converted to ThO2 by moisture in ionic liquid
    Dalton Trans, 24, 4532-4534 (2002)
Role of water central, useful in dissolution by problematic in full reduction

## Slide 56: Choice of Ionic Liquid
A number of ionic liquids initially investigated
bis(trifluoromethanesulfonyl)imide (TFSI) anion selected for study at UNLV
  Functionalized TFSI evaluated
    propyl and imidazolium
  large potential window with Au, Pt, and Glassy carbon electrodes
    Suitable for reduction of lanthanides and actinides
Ionic liquid
  N-trimethyl-N-butylammonium bis(trifluoromethanesulfonyl)imide
    Used with actinides
  Written as [Me3NBu][TFSI]

## Slide 57: Electrochemistry in ionic liquids
ILs have wider potential window
  Actinide electrochemistry possible
  Must limit water in the system
TFSI is a poor ligand
  Moves deposition to favorable potential
Electrode can influence window
  Glassy Carbon (GC) widest potential window

## Slide 58: U TFSI compound synthesis
All reactions were performed in an argon filled glove box
K(TFSI)(s) synthesized by adding H(TFSI) and KH THF solution
  K(TFSI) separated by decanting excess THF
    90% yield
K(TFSI) and UI3(THF)4 dissolved in THF
  Excess of K(TFSI) added to ensure reaction completion
  Clear pale yellow solution was stirred for 24 hours
  Final orange red solution
    Contained off white KI solid precipitate
    THF solution contained product U(TFSI)3
    Solid was isolated by evaporating excess THF
      74% yield

## Slide 59: Formation of Uranium Deposits
Constant potential of -1.5 V versus NHE
SEM, EDS, and XRD analysis performed
SEM of U deposited on Au foil
XRD evaluation of sample
  Alpha U metal
SEM EDS
  No oxygen at 5.5 keV
Au electrode
U-metal deposit

## Slide 60: Direct dissolution of U3O8 into ionic liquid
Original dissolution conditions:
45 mg U3O8 with 3.27 M HTFSI in Me3NBuTFSI Stirred for weeks with no change
RESULT: dissolution of material
oxidizing gas used
  O3, NO2
Addition of HTFSI
  Promote formation of uranium-TFSI complex
Ozone
(From compressed air)
t = 24 hrs

## Slide 61: Direct dissolution of U3O8 into RTIL
Proposed dissolution mechanism:
U3O8 + 6 HTFSI + O3 3 UO22+ + 6 TFSI- + 3 H2O + O2
Supporting EXAFS data of the original dissolution solution
confirmed presence of UO22+
coordinated with five to six equatorial oxygens.
2 O @ 1.75 Å
6 ± 1 O @ 2.38 Å
U --- O multi scattering @ 3.56 Å

## Slide 62: RDCH 702: Lecture 9 Separations Part 3
Separation methods
  Solvent extraction
    PUREX
  Ion exchange
  Volatility
  Electrochemistry
Specific actinide separations
Basic concept of separations
  Oxidation state
  Ionic radius
Development of advanced separations
  Trivalent actinides
Necessary for fuel cycle due to formation of mixtures due to fission
  Actinides
    Transuranics
  Fission products
    Se (Z=34) to Dy (Z=66)
Tributyl phosphate (TBP)

## Slide 63: RDCH 702: Lecture 9 Separations Part 4
Separation methods
  Solvent extraction
    PUREX
  Ion exchange
  Volatility
  Electrochemistry
Specific actinide separations
Basic concept of separations
  Oxidation state
  Ionic radius
Development of advanced separations
  Trivalent actinides
Necessary for fuel cycle due to formation of mixtures due to fission
  Actinides
    Transuranics
  Fission products
    Se (Z=34) to Dy (Z=66)
Tributyl phosphate (TBP)

## Slide 64: Pu separations
1855 MT Pu produced
  Current rate of 70-75 MT/years
  225 MT for fuel cycle
  260 MT for weapons
Large scale separations based on manipulation of Pu oxidation state
  Aqueous (PUREX)
  Non-aqueous (Pyroprocessing)
Precipitation methods
  Basis of bismuth phosphate separation
    Precipitation of BiPO4 in acid carries tri- and tetravalent actinides
      Bismuth nitrate and phosphoric acid
      Separation of solid, then oxidation to Pu(VI)
    Sulfuric acid forms solution U sulfate, preventing precipitation
  Used after initial purification methods
  LaF3 for precipitation of trivalent and tetravalent actinides

## Slide 65: Pu separations
Solvent extraction
  TBP extraction, PUREX process
    Some interest in 3rd phase formation
Extraction chromatography
  Extractant on solid support
Ion-exchange
  Both cation and anion exchange
    Anion exchange based on formation of appropriate species in acidic solution
    Change of solution impact sorption to column
Pu separation
  Sorb Pu(IV,VI) in 6 M acid, reduce to Pu(III)
General cation exchange trends for Pu
  HNO3, H2SO4, and HClO4 show stronger influence than HCl
  Strong increase in distribution coefficient in HClO4 at high acidities exhibited for Pu(III) and Pu(VI)
Anion exchanges in high acid, formation of charged species

## Slide 66: Pu separations
Halide volatility (PuF6, PuCl6)
  PuO2 in fluidized bed reactor with fluorine at 400° C
    Can substitute NH4HF2 for some fluorination
    Also use of O2F2
  PuF6 decomposes to PuF4 and F2 in a thermal decomposition column
Supercritical fluid extraction
  Most research with CO2
  Use complexants dissolved in SCF
    TBP.HNO3, TTA for extraction from soil
  Change of pressure to achieve separations

## Slide 67: Pu separations
Alkaline solutions
  Need strong ligands that can compete with hydroxide to form different species
    F-, CO32-, H2O2
      High solubility, based on oxidation state
      Stabilize Pu(VII)
Room temperature ionic liquids
  Quaternary ammonium with anions
    AlCl4-, PF6-
  Liquid-liquid extraction
  Electrochemical disposition
N
S
S
O
O
O
O
C
F
3
F
3
C

## Slide 68: Am solvent extraction
Tributylphosphate (TBP)
  Am extracted from neutral or low acid solutions with high nitrate
  Am(VI)
    Oxidation with (NH4)10P2W17O61 to stabilize Am(VI)
    100 % TBP from 1 M HNO3
      Separation factor 50 from Nd
  Am separation from lanthanides
    1 M ammonium thiocyanate aqueous phase
Dibutyl butylphosphonate (DBBP)
  Phosphonate functional group
  Similar to TBP, stronger extractant of Am
Trialkylphophine oxide (TRPO)
  Increase in basicity of P=O functional group from TBP to DPPB to TRPO
  Am and Cm extraction from 1-2 M HNO3
  30 % TRPO in kerosene
    Am, Cm, tetravalent Np and Pu, hexavalent U extracted
      Actinides stripped with 5.5 M HNO3 (Am fraction)
    TRPO with C6-C8 alkyl group

## Slide 69: Am solvent extraction
HDEHP
Bis(2-ethylhexyl)phosphoric acid (HDEHP)
  Has been used to Am separation
  Part of TALSPEAK
    Extracts lanthanides stronger that actinides
    TALSPEAK components
      Bis(2-ethyl-hexyl)phosphoric acid (HDEHP)
      HNO3
      DTPA
      Lactic acid
Carbamoylphosphine oxide (CMPO)
  Synthesized by Horwitz
    Based on DHDECMP extractions
      Recognized functional group, simplified ligand synthesis
      Purified by cation exchange
  Part of TRUEX
    TRUEX (fission products)
      0.01 to 7 M HNO3
      1.4 M TBP
      0.2 M Diphenyl-N,N-dibutylcarbamoyl phosphine oxide (CMPO)
      0.5 M Oxalic acid
      1.5 M Lactic acid
      0.05 M DTPA
CMPO

## Slide 70: Am solvent extraction
Tertiary amine salt
  Low acid, high nitrate or chloride solution
    (R3NH)2Am(NO3)5
Quaternary ammonium salts (Aliquat 336)
  Low acid, high salt solutions
    Extraction sequence of Cm<Cf<Am<Es
  Studies at ANL for process separation of Am
Amide extractants
  (R1,R2)N-C(O)-CR3H-C(O)-N(R1R2)
    Diamide extractant
    Basis of DIAMEX process
  N,N’-dimethyl-N,N’-dibutyl-2-tetradecyl-malonamide (DMDBTDMA)
    DIAMEX with ligand in dodecane with 3-4 M HNO3
      Selective extraction over Nd

## Slide 71: Am/Ln solvent extraction
Extraction reaction
  Am3++2(HA)2AmA3HA+3 H+
    Release of protons upon complexation requires pH adjustment to achieve extraction
      Maintain pH greater than 3
Cyanex 301 stable in acid
  HCl, H2SO4, HNO3
    Below 2 M
Irradiation produces acids and phosphorus compounds
  Problematic extractions when dosed 104 to 105 gray
New dithiophosphinic acid less sensitive to acid concentration
  R2PSSH; R=C6H5, ClC6H4, FC6H4, CH3C6H4
    Only synergistic extractions with, TBP, TOPO, or tributylphosphine oxide
    Aqueous phase 0.1-1 M HNO3
    Increased radiation resistance
Distribution ratios of Am(III ) and Ln(III ) in 1.0 M Cyanex 301‐heptane (16 mol% of Cyanex 301 neutralized before extraction contacts)

## Slide 72: Ion exchange separation Am from Cm
LiCl with ion exchange achieves separation from lanthanide
Separation of tracer level Am and Cm has been performed with displacement complexing chromatography
  DTPA and nitrilotriacetic acid in presence of Cd and Zn as competing cations
  displacement complexing chromatography method is not suitable for large scale
Ion exchange has been used to separate trace levels of Cm from Am
  Am, Cm, and lanthanides sorbed to a cation exchange resin at pH 2
    Separation of Cm from Am was performed with 0.01 % ethylenediamine-tetramethylphosphonic acid at pH 3.4 in 0.1 M NaNO3
    separation factor of 1.4
Separation of gram scale quantities of Am and Cm by cation and anion exchange
  use of a-hydroxylisobutyrate or diethylenetriaminepentaacetic acid as an eluting agent or a variation of eluant composition by addition of methanol to nitric acid
    best separations were achieved under high pressure conditions
      separation factors greater than 400
Distribution
coefficients of actinides and lanthanides into Dowex 1 8 resin from 10 M LiCl

## Slide 73: Extraction chromatography
Mobile liquid phase and stationary liquid phase
  Apply results from solvent extraction
    HDEHP, Aliquat 336, CMPO
      Basis for Eichrom resins
      Limited use for solutions with fluoride, oxalate, or phosphate
    DIPEX resin (Eichrom)
      Bis-2-ethylhexylmethanediphosphonic acid on inert support
      Lipophilic molecule
        Extraction of 3+, 4+, and 6+ actinides
      Strongly binds metal ions
        Need to remove organics from support
  Variation of support
    Silica for covalent bonding
    Functional organics on coated ferromagnetic particles
      Magnetic separation after sorption

## Slide 74: Am separation and purification
Precipitation method
  Formation of insoluble Am species
    AmF3, K8Am2(SO4)7 , Am2(C2O4)3, K3AmO2(CO3)2
      Am(V) carbonate useful for separation from Cm
      Am from lanthanides by oxalate precipitation
        Slow hydrolysis of dimethyloxalate
        Oxalate precipitate enriched in Am
        50 % lanthanide rejection, 4 % Am
  Oxidation of Am(VI) by K2S2O8 and precipitation of Cm(III)
Pyrochemical process
  Am from Pu
    O2 in molten salt, PuO2 forms and precipitates
    Partitioning of Am between liquid Bi or Al and molten salts
      Kd of 2 for Al system
    Separation of Am from PuF4 in salt by addition of OF2
      Formation of PuF6, volatility separation

## Slide 75: Cm separation and purification: Similar to Am
Solvent extraction
  Organic phosphates
    Function of ligand structure
      Mixed with 6 to 8 carbon chain better than TBP
  HDEHP
    From HNO3 and LiCl
  CMPO
    Oxidation state based removal with different stripping agent
  Extraction of Cm from carbonate and hydroxide solutions, need to keep metal ions in solution
    Organics with quaternary ammonium bases, primary amines, alkylpyrocatechols, b-diketones, phenols
Ion exchange
  Anion exchange with HCl, LiCl, and HNO3
    Includes aqueous/alcohol mixtures
    Formation of CmCl4- at 14 M LiCl
      From fluorescence spectroscopy
Precipitation
  Separation from higher valent Am
    10 g/L solution in base
    Precipitation of K5AmO2(CO3)3 at 85 °C
    Precipitation of Cm with hydroxide, oxalate, or fluoride

## Slide 76: Review
Understand the differences and techniques for
  Solvent extraction
  Ion exchange
  Electrochemistry
  Volatility
Understand how oxidation state influences different separation methods
Understand the different mechanisms in solvent extraction
Compare and contrast specific actinide separation
Describe the components of an ion exchange resin
Provide a ion exchange and solvent extraction separation for Am from the other actinides.
Provide the basic of electrochemical and IL separations.
  What is the differences in these methods?

## Slide 77: Questions
Describe the concepts in solvent extraction?
What is third phase formation in solvent extraction?
  How can it be controlled?
  What is third phase important to understand for actinide separations?
  How can it be exploited in chemistry?
Describe a volatility based separation for Pu.

## Slide 78: PDF Quiz
Respond to Lecture 9 PDF quiz
Provide comment on blog